SPECIFICATIONS LOGGIAWOOD®

Manufacturer	: RENSON LOGGIA® SLIDING PANELS

Type 			: LOGGIAWOOD® PARO 0160 WITH FRAME LG.040 (PA-G-5.0720)

Description:

RENSON LOGGIAWOOD® PARO 0160 is a sliding panel made up of a combination of various materials used to manage heat entry and natural daylight. The concept combines the typical characteristics of extruded aluminium – in a strong circumferential frame LG.060 with a surface treatment specified by the architect – and the naturalness of wood as panel infill. The unique wooden blade fastening technique – without visible joints – allows for a smooth dilatation of the blades in the frame profile, without any vibration noise. If requested an FSC or PEPC timber label (guarantee for sustainable logging) can be supplied.

Standards :

- Aluminium-Alloy : Al Mg Si 0,5 (F25)

- Standard : EN AW-6063

- Curing : T66

- Aluminium pre-treatment :

- Norm DIN 5002155

- Strength calculations are based on the following standards :

- ENV 1999-1-1 : Calculations of aluminium constructions

- NBN B-03-002-2 : Wind load – Dynamic effects

- EN 1991-1-4 : Wind load

- Panel meets all CE requirements as stated in the performance declaration DoP/RP/001 on the basis of harmonised technical specifications according to EN 13659:2004.

- Surface treatment – aluminium :

- Anodized natural colour finish F1 (20 micron) : pre-treated and anodized

- Polyester powder paint in RAL-colours (60 to 80 micron) : aluminium profiles corrosion resistance pre-treated (DIN 5002155) to guarantee a firm powder coating, after which thermally painted

Implementation system :

- Frame :

- Vertical frame profiles LG.060.01, laterally provided with a cover profile LG.060.02 for level view, made from extruded aluminium.

  - Dimensions of the frame profile  :

    - Width : 40 mm

    - Depth : 60 mm

    - Minimum inertia moments Iy = 74.209 mm4 (strong axis) ;  Iz = 268.228 mm4, where a minimal material thickness of  2,0 mm

- Depending on the height of the sliding panel the horizontal frame profile (above and/or below) can measure 70 mm in height instead of 40 mm.

  - Horizontal frame profile LG.040.09 :

    - Depth : 40 mm

    - Height : 40 mm

    - Minimum inertia moments Iy = 75.158 mm4 (strong axis) ;  Iz = 72.301 mm4, where a minimal material thickness of 2,0 mm

  - Horizontal frame profile LG.040.70 :

    - Depth : 40 mm

    - Height : 70 mm

    - Minimum inertia moments Iy = 317.123 mm4 (strong axis) ;  Iz = 116.033 mm4, where a minimal material thickness of  2,0 mm

- Invisible corner joints by means of cover profile and covers.

- Blades :

- Parallelogram shaped wooden blades WRC.PL.065

- High quality wooden blades of WRCedar Clear n°2 – untreated, suitable for natural aging

- Dimensions :

    - Height :  16 mm

    - Depth : 65 mm

    - Critical angle for incoming sun rays : 47°

    - Perpendicular visual opening : 29 mm

    - Step : 90 mm (11 blades at 1 meter high)

    - Blade angle : 57° (relative to the vertical direction)

    - Minimum inertia moments Iy = 223.630 mm4 (strong axis) ;  Iz = 15.126mm4

- Blades incorporated discreetly and without visible fixings in the vertical side profiles of the frame

- The fastening technique allows for a smooth dilatation of the blades in the frame profile, without any vibration noise

- Slide fittings :

- High quality maintenance free sliding fittings, comprise of : sliding rail (above) with trolley / suspension bracket and adjustable railstop; guiding system (under) aluminium L-profile 20/20/4 and plastic guiding system ; lateral rubberstop to prevent damage to the panel

- Movement capabilities of the sliding panel (according to chosen design) : simple - or symmetrical sliding

- Motorised control - according to chosen design :

    - 230V motor – for connection to simple switch or buildings control system

- Slide fittings “CE” approved

- System features :

- Combination of sturdy aluminium frame and naturally durable wooden blades made of Western Red Cedar

- Frame profile with completely view and invisible inner corner joints

- Depending on the height of the sliding panel the horizontal frame profile (above and/or below) can measure 70 mm in height instead of 40 mm

- Dimensions :

- Maximum possible dimensions depend on local wind load “qb”

- Optional accessories :

- Flexible under guiding system Flexguide®: self-regulating under guiding system for sloping areas with L-, T of U-shaped (incorporated) under guiding systems profile – see separate specifications.