SPECIFICATIONS LOGGIAWOOD®

Manufacturer	: RENSON LOGGIA® SLIDING PANELS

Type 		    : LOGGIAWOOD® PARO 0160 PRIVACY (PA-G-5.0730)

Description :

RENSON LOGGIAWOOD® PARO 0160 PRIVACY combines the quality of aluminium and the naturalness of wood in an aesthetically pleasing, efficient and current system. With the “Privacy” concept the blades are moveable and as such can be manually tilted from a closed to a fully open position or vice versa. The sturdy circumferential frame of extruded aluminium, guarantees a good dimensional stability as a whole, whilst the wooden blades lend the panels a very natural and elegant look. If requested an FSC or PEPC timber label (guarantee for sustainable logging) can be supplied.

Standards :

- Aluminium-Alloy : Al Mg Si 0,5 (F25)

- Standard : EN AW-6063

- Curing : T66

- Aluminium pre-treatment :

- Norm DIN 5002155

- Strength calculations are based on the following standards :

- ENV 1999-1-1 : Calculations of aluminium constructions

- NBN B-03-002-2 : Wind load – Dynamic effects

- EN 1991-1-4 : Wind load

- Panel meets all CE requirements as stated in the performance declaration DoP/RP/001 on the basis of harmonised technical specifications according to EN 13659:2004.

Surface treatment – aluminium :

- Anodized natural colour finish F1 (20 micron) : pre-treated and anodized

- Polyester powder paint in RAL-colours (60 to 80 micron) : aluminium profiles corrosion resistance pre-treated (DIN 5002155) to guarantee a firm powder coating, after which thermally painted

Implementation system :

- Frame :

- Vertical frame profiles LG.060.01, laterally provided with a cover profile LG.060.02 for level view, made from extruded aluminium.

  - Dimensions of the frame profile  :

    - Width : 40 mm

    - Depth : 60 mm

    - Minimum inertia moments Iy = 74.209 mm4 (strong axis) ;  Iz = 268.228 mm4, where a minimal material thickness of  2,0 mm

- Depending on the height of the sliding panel the horizontal frame profile can measure 55 mm high at the top instead of 40 mm and 70 mm below instead of 40 mm.

  - Horizontal frame profile LG.040.09 :

    - Depth : 40 mm

    - Height : 40 mm

    - Minimum inertia moments Iy = 75.158 mm4 (strong axis) ;  Iz = 72.301 mm4, where a minimal material thickness of 2,0 mm

  - Horizontal frame profile LG.040.55 :

    - Depth : 40 mm

    - Height : 55 mm

    - Minimum inertia moments Iy = 169.579 mm4 (strong axis) ;  Iz = 91.248 mm4, where a minimal material thickness of  2,0 mm

  - Horizontal frame profile LG.040.70 :

    - Depth : 40 mm

    - Height : 70 mm

    - Minimum inertia moments Iy = 317.123 mm4 strong axis) ;  Iz = 116.033 mm4, where a minimal material thickness of 2,0 mm

- Invisible corner joints by means of cover profile and covers.

- Blades

- Parallelogram shaped wooden blades WRC.PL.065, suitable for manual tilting from a closed to open position or vice versa with two control settings, which allows for one section to be closed and the other open.

- High quality wooden blades of WRCedar Clear n°2 – untreated, suitable for natural aging

- Dimensions :

    - Height :  16 mm

    - Depth: 65 mm

    - Step : 57 mm (17 blades at 1 meter high)

    - Minimum inertia moments Iy = 223.630 mm4 (strong axis) ;  Iz = 15.126mm4

- Sliding fittings :

- High quality maintenance free sliding fittings, comprise of : sliding rail (above) with trolley / suspension bracket and adjustable railstop; guiding system (under) aluminium L-profile 20/20/4 and plastic guiding system ; lateral rubberstop to prevent damage to the panel

- Movement capabilities of the sliding panel (according to chosen design) : simple - or symmetrical sliding

- Motorised control – according to chosen design :

    - 230V motor – for connection to simple switch or buildings control system

- Sliding fittings “CE” approved

- System features :

- Blades manually tilt, from closed position to fully open or vice versa in two control settings.

- Frame profile with level view and invisible internal corner joints

- Depending on the height of the sliding panel the horizontal frame profile can measure 55 mm high at the top instead of 40 mm and 70 mm below instead of 40 mm

- Dimensions :

- Maximum possible dimensions depend on local wind load “qb”

- Optional accessories :

- Flexible under guiding system Flexguide®: self-regulating under guiding system for sloping areas with L-, T or U-shaped (incorporated) under guiding systems profile – see separate specification.