## Specifications sheet

**Material**  
» Units are assembled from extruded sections of Aluminium Al Mg Si 0,5  
  
**Finishing**  
» Natural or bronze anodised: 20 to 22 micron  
» Powder-coated in any RAL-colour  
» Galvanised steel sleeve  
  
**Description**  
» The galvanised steel sleeve which is fitted to the internal louvre, can be adapted for any thickness of wall (24,5 - 40 cm)  
» An insect screen in stainless steel (18/8) is fitted as standard.  
» The galvanised steel sleeve can be adapted for any thickness of wall (245 mm X 400 mm).  
» Net airflow : 38 cm².  
» Dimensions: 256 X 90 mm (W X H)  
» Sound absorbing application possible.