## Specifications sheet

Material
» Aluminium Al Mg Si 0,5

Finishing
» Natural anodised: 20 to 22 micron
» Powder-coated in any RAL-colour: pre-assembled product is conversed to ensure a solid adherence (Brugal) and powder-coated in order to guarantee a thorough powder-layer at all corner joints and cutting sections: 60 to 70 micron.

Description
» Frame profiles with a total height of 19,5 mm cut at mitre of 45° and assembled through compression and a clamping corner.
» Length of blades: max. 800 mm in one piece.
» The V-shaped blades have a height of 20 mm.
» The pitch of the blades is 20 mm.
» Supplied with matching back frame and fixing screws.

Specification
» Suitable for door thickness of min. 30 and max. 54 mm.
» Flange size frame: 15 mm
» Maximum width in one piece: 800 mm

Fixing
» Screws are supplied as standard.