## Specifications sheet

Material
» Aluminium Al Mg Si 0,5

Finishing
» Natural anodised : 12 to 15 micron
» Bronze anodised : 12 to 15 micron
» Champagne anodised : 12 to 15 micron
» Gold anodised : 12 to 15 micron
» Powder-coated in any RAL-colour: pre-assembled product is chromatised and powder-coated in order to guarantee a thorough powder-layer at all corner joints and cutting sections.

Description
» Aluminium blades with a diameter of 20 mm X 4 mm.
» Pitch between the blades is 12,5 mm.
» The grille is manufactured in multiple sections of +/- 1 metre.
» Frames: maximum 3500 mm, provided with an acoustic seal strip.
» The frame is assembled from a 'L' or 'Z' shaped profile or without frame.
» Frame height: 25 mm (over all width)

Applications
» Grilles for drains in swimming pools, basement car parks, abattoirs, etc.
» Grilles to cover the underground cabling in computer rooms.

Fixing
» Dowels no. 231 are supplied to fix the louvre.