## Specifications sheet

Material
» Aluminium Al Mg Si 0,5

Finishing
» Natural anodised: 20 to 22 micron
» Dark bronze anodised: 20 to 22 micron
» Champagne anodised: 20 to 22 micron
» Gold anodised: 20 to 22 micron
» Powder-coated in any RAL-colour: pre-assembled product is chromatised and powder coated in order to guarantee a thorough powder-layer at all corner joints and cutting sections: 60 to 70 micron.

Description
» Aluminium bars with a diameter of 16X3 mm and a 15° deflection
» Free area of 75%
» Standard wide bars on 10 mm centres
» The frame is assembled from extruded sections of maximum 1600X300 mm
» Frame: maximum length: 3500 mm
» Types:
» 'Z'-frame (W X H) (16 X 19,5 mm) (5 mm surface mounted) narrow 'Z'-frame (W X H) (20,5 X 15,25 mm) (1,5 mm surface mounted) without frame

Applications
» Grille for heating.