**Specifications sheet**

**Material**
» Aluminium Al Mg Si 0,5

**Finishing**
» Natural anodised: 20 to 22 micron
» Dark bronze anodised: 20 to 22 micron
» Powder-coated in any RAL-colour: pre-assembled product is conversed to ensure a solid adherence (Brugal) and powder-coated in order to guarantee a thorough powder-layer at all corner joints and cutting sections: 60 to 70 micron.

**Description**
» Aluminium profiles with a minimum thickness of 1,5 mm.
» Aluminium blades are fixed in the vertical profiles by means of an axle perforated through the blade enabling the blade to rotate.
» The blades for extractor hoods (173X173 mm and 210X210 mm and 246X246 mm) are mutually joined and go open/close together, to reduce noice nuisance.

**Specification**
» Thickness: 29 mm
» Sizes possible in height: 228 mm; 100 mm increments of height
» The blades have a maximum length of 800 mm in one piece.

**Fixing**
» Screws and plugs are supplied.