**Specifications sheet**

**Material**  
» Aluminium Al Mg Si 0,5  
  
**Finishing**  
» Natural anodised: 20 to 22 micron  
» Dark bronze anodised: 20 to 22 micron  
» Powder-coated in any RAL-colour: pre-assembled product is conversed to ensure a solid adherence (Brugal) and powder-coated in order to guarantee a thorough powder-layer at all corner joints and cutting sections: 60 to 70 micron.  
  
**Description**  
» Aluminium profiles with a minimum thickness of 1,5 mm.  
» Aluminium blades are fixed in the vertical profiles by means of an axle perforated through the blade enabling the blade to rotate.  
» The blades for extractor hoods (173X173 mm and 210X210 mm and 246X246 mm) are mutually joined and go open/close together, to reduce noice nuisance.  
  
**Specification**  
» Thickness: 29 mm  
» Sizes possible in height: 228 mm; 100 mm increments of height  
» The blades have a maximum length of 800 mm in one piece.  
  
**Fixing**  
» Screws and plugs are supplied.