## Specifications sheet

**Material**  
» Aluminium Al Mg Si 0,5  
  
**Finishing**  
» Powder-coated in RAL 9010, 8019, 9006 (aluminium finish) on chromatised (Brugal= environmental alternative to chromatic treatment) underground of 60 to 70 micron or in any other RAL-colour.  
  
**Description**  
» Extraction and air supply with round frame.  
» Aluminium flyscreen.  
» Aluminium plate with a thickness of 1,5 mm.  
» Fixed diameters of 95, 115, 145, 190 and 245 mm for tubes of respectively 100, 120, 150, 200 and 245 mm.  
  
**Fixing**  
» Standard sizes with extensible brackets.  
» Spring clips are supplied with diameters  
95 mm (PVC-tube 110 mm)  
145 mm (PVC-tube 160 mm)