## Specifications sheet

Material 
» Aluminium Al Mg Si 0,5

Finishing 
» Natural anodised: 20 to 22 micron !Dark bronze anodised: 20 to 22 micron 
» Powder-coated in any RAL-colour: pre-assembled product is chromatised and 
powder-coated in order to guarantee a thorough powder-layer at all joints and cutting sections : 60 to 70 micron 

Description 
» L-shaped window profile welded at 1 point.
» Z-shaped blades with a with a height of 33,3 mm and with a distance of 19,3 mm. 
» An anti-static and stainless steel insect mesh (18/8) is fitted flush on the back of the louvre by means of a nylon cord. 

Specification 
» Minimum diameter : 300 mm. 
» Maximum diameter : 1400 mm. when anodised in natural (F1) 1500 mm. when powder coated in a RALcolour In two parts as from 1500 mm. diameter 
» Depth to fit : 28 mm. 
» Visual free area : 50 % 

Fixing 
» Dowels nr. 428 are supplied to fix the louvre