## Specifications sheet

Material & finishing:
• Aluminium AlMgSi 0,5
• Natural anodised: 20 à 22 micron (UK: 25 micron)
• Powder-coated in any RAL-colour possible: chromatised first and then powder-coated (60 à 70 micron)

Description:
• L-shaped window profiles with a total height of 64 mm cut at mitre of 45° and assembled through compression and a clamping corner.
• Aluminium blade supports are rivetted on the vertical perforated frame-profiles.
• Louvres with a width over 700 mm are provided with an extra perforated U-profile to fix additional blade supports in order to strengthen the whole construction.
• The blades are clipped onto the support profiles. Distance between the blades is 54 mm.
• An anti-static and stainless steel 316 insect mesh 6 x 6 mm is fitted flush on the back of the louvre by means of a nylon cord.

Dimensions & technical data:
• Depth to fit : 81,5 mm
• Blade pitch : 60 mm
• Flange size : 50 mm
• Total thickness : 86,5 mm
• Physical free area : 76%
• Visual free area : 90%

Options:
• Waterchannel
• Fixed just under the lowest blade to ensure a better water drainage
• This water channel is made of Aluminium Al Mg Si 0,5 and anodised or powder-coated in any RAL-colour in the same finish as the louvre.
• Insect mesh (flyscreen)
• Stainless steel 316 insect mesh, 2.3 x 2.3 mm fitted flush on the back of the louvre by means of a nylon cord.

Fixation:
• Dowels no.429 are supplied to fix the louvre.