## Specifications sheet

**Material**  
» Aluminium Al Mg Si 0,5  
  
**Finishing**  
» Natural anodised: 20 to 22 micron  
» Dark bronze anodised: 20 to 22 micron  
» Powder-coated in any RAL-colour: pre-assembled product is chromatised and powder-coated in order to guarantee a thorough powder-layer at all corner joints and cutting sections: 60 to 70 micron.  
  
**Description**  
» Frame-profiles with a total height of 29 mm.  
» Aluminium blade supports are rivetted on the vertical perforated frame-profiles.  
» Louvres with a width over 700 mm are provided with an extra perforated Uprofile to fix additional blade supports in order to strenghten the whole construction.  
» The Z-shaped blades with a height of 33,5 mm are clipped onto the support profiles.  
» The pitch of the blades is 20 mm.  
» An anti-static and stainless steel insect mesh 304 (2,3 X 2,3 mm) is fitted flush on the back of the louvre by means of a nylon cord.  
  
**Specification**  
» Depth: 29 mm  
» Minimum profile thickness: 1,5 mm  
» Visual free area: 59%  
  
**Fixing**  
» Screws and plugs are included.